Product Information Sheet

Daycon Products Company, Inc.   16001 Trade Zone Avenue, Upper Marlboro, MD 20774

Local: (301) 218-1000  Toll Free: (800) 394-0019  Fax (301) 218-7191

This sheet is not a Safety Data Sheet (S.D.S.), nor does it satisfy the requirements to have one.  All information on this sheet is believed to be accurate, but no warranty is expressed or implied.  The product described herein is for use only by trained, professional, cleaning personnel.

CRYSTAL BRITE

Environmentally Responsible Floor Finish

Description:		Daycon Crystal Brite is certified by Green Seal™ to meet their GS-40 environmental standard for Industrial and Institutional floor care products based on its reduced human and aquatic toxicity and reduced smog production potential. Crystal Brite is a sealer/finish that exhibits excellent durability and burnish response. It is zinc-free and alkyl phenyl ethoxylate (APE) free. It contains no phthalates, and is low in VOC content. It has excellent scuff, scratch and heel mark resistance, and retains a high gloss under heavy traffic conditions. Crystal Brite meets or exceeds the CSPA and UL slip resistance standard of 0.5 minimum as tested on a James Machine by an outside laboratory in accordance with ASTM D2047-99 or UL Method 410.

Green Certification Statement: This product meets Green Seal™ Standard GS-40 based on effective performance and protective limits on VOCs and human & environmental toxicity. GreenSeal.org.

Benefits:

      - GS-40 Certified

      - Contains no zinc or other heavy metals.

      - Self cross linking

      - Sealer/Finish

      - Contains no alkyl phenyl ethoxylates (APE)

      - Contains no phthalates

      - Low VOC

      - High initial gloss

      - Extremely durable

      - Extremely clear finish

      - Does not yellow

      - May be dry burnished

Specifications:

Appearance:			Opaque liquid

Color:				White

Odor:				Mild acrylic

Total Solids			20% minimum

Use dilution:			As is

Coverage (First coat)		1500-2000 sq. ft./gal

Coverage (Recoating)		2000-2500 sq. ft./gal.

Storage Stability:		Two years minimum in sealed container

Protective Clothing:		See Safety Data Sheet (SDS)

VOC, % as is:			4 (equivalent to about 40 gm/l)

Product Conformance:		Manufactured by an ISO 9001:2008 registered company.

Comments:		Only a neutral cleaner such as Kleer ‘n Brite should be used for normal maintenance. Crystal Brite can be removed with Daycon Meteor. It has excellent dry burnish response with a beige pad.

Directions:		Top scrub the floor with a peach or blue pad using a solution of 1 oz. per gallon of Kleer ‘N Brite Neutral Cleaner. After top scrubbing, burnish the floor with a beige pad, or natural hair pad followed by a beige pad if the floor has excessive scratching, then apply 3-4 coats of Crystal Brite. If the current level of floor finish is beyond repair, first strip the floor using Daycon’s Meteor (GS-40 Compliant Stripper). After stripping, rinse with a solution of 1 oz. Kleer ‘N Brite per gallon of water. To ensure all stripper is picked up, rinse the floor at least two times. The floor may then be recoated with 3-5 coats of Crystal Brite. Maintain Crystal Brite with a dust mop, a damp mop with neutral cleaner, and a beige pad to burnish. Floor should be dry burnished until the finish stops responding. To help restore gloss, burnish using Maintainer Plus, Sunrise, Burnishing Gel #27, or R-T-U Express.

Product Disposal: 	This product is non-hazardous material. Dispose of in accordance with local, state, and federal regulations. It is recommended that the high density polyethylene container and any corrugated packaging be recycled.

Packed:

| Packaging/Description | Item Code |
| --- | --- |
| Gallon (4 per case) | 628909 |
| 5 Gallon Pail | CRYSTAL5GAL |

Date:		         October 29, 2013